# Tip Outs

The largest of the so-called tip out areas is the bathroom.

It is 15 sqft.  At 40 lbs/sqft that is a total live load of 604 lbs.  The dead load is some 200 lbs for a total of 804 lbs.

That load is centered 18” from the center of the wall that supports it.

That moment is thus 1206 ftlbs. or 14472 inlbs.

By summation of moments, the horizontal load pulling away from the wall at the top is 172 lbs.

The entire perimeter of the join has biaxial roving inside and out.  For simplicity, we will only count the top surface in the calculations.

Recall that the biaxial roving has a bending strength of 40,000 psi and a shear strength of 3,000 psi.  Understand that is for every inch of the perimeter of every part, inside and out.

If only bonded at the top, 68”, with half of a typical 6” biaxial tape, you get 204 sqin. of laminate contact.  At 3000 psi, that gives 612,000 lbs.  For simplicity lets use just 1000 lbs/sqin.  That is 204,000 lbs.  BUT that is only one side.  Every panel is bonded on both sides.  Double that 204K.  That is 408K lbs.

That safety factor is of how many hundred?